## Slide 1
A new strategy for fatigue analysis in presence of general multiaxial time varying loadings
Zepeng MA, Patrick Le Tallec, Habibou Maitournam
Laboratory of Solid Mechanics, Ecole Polytechnique, 91128 Palaiseau Cedex, France
The object of this work is to propose an energy based fatigue approach which takes into account impurities and hardness in the material.
The proposal of our model is to consider a plastic behavior at the mesoscopic scale with a dependence of the yield function not only on the deviatoric part of the stress but also on the hydro static part.
A kinematic hardening under the assumptions of associative plasticity is also considered.
  Our fundamental thought is to assume that the local dissipated energy at small scale governs fatigue at failure.
  The structure is elastic at the macroscopic scale. At each material points, there is a stochastic distribution of weak points which will undergo strong plastic yielding, which contribute to energy dissipation without affecting the overall macroscopic stress.
  Instead of using the number of cycles, we use the concept of loading time. We also take into account the nonlinearity of damage accumulation.
BACKGROUND
PROPOSE
Weakening scales
We assume the weakening scales have a probability distribution of power law:
  1. Elastic regime, in phase 2 and 4, there is , then
  Plastic regime according to plastic flow rule, with increasing plastic deformation, in phase 5 and 1, there is
  with , then and
  Plastic regime in the other direction, in phase 3, there is , then and
Integration rules for energy dissipation rate and damage
Instead of doing the scale integration directly which can be difficult for complex loading, the Gaussian Quadrature rule with Legendre points is used to give the value of local dissipated energy rate.
METHODS AND ANALYSIS
M. Maitournam, C. Krebs, A. Galtier, A multiscale fatigue life model for complex cyclic multiaxial loading, International Journal of Fatigue.
S. Bosia, A. Constantinescu, Fast time-scale average for a mesoscopic high cycle fatigue criterion, International Journal of Fatigue.
J. Lemaitre, J.-L. Chaboche, Mechanics of solid materials, Cambridge university press, 1990.
Legendre Gauss Quadrature weights and nodes, https://www.mathworks.com/matlabcentral/fileexchange/4540-legendre-gauss-quadrature-weights-and-nodes, accessed: 2004-05-11.
Email : zepeng.ma@polytechnique.edu. This research supported by PSA group.
Figure 1: and evolution with time under different weakening scales in sinusoidal load.
3D real data loading test
CONCLUSIONS
REFERENCES
Simple cyclic loading test
The strategy can be made more complex by introducing a local space averaging process in the calculation of the local damage, and by taking more general plastic flows. The energy based fatigue approach takes into account impurities and hardness in the material which affect the fatigue life. The load sequence effects for complex multiaxial loading history are included in damage accumulation process. The small step-by-step strategy does not ignore small fluctuations in the load history. In addition, it can take into account any type of micro plasticity law and multiaxial load geometry.
Figure 4: Circled area magnification in Figure 4 where in the circled area there is.
Figure 3: and evolution with time under different weakening scales in PSA load history.
Figure 2:Damage evolution with time under sinusoidal load with two different methods.